Performance Specification

| Model |  |  | Vmax | Vmax |  |  | Maximum Time |  | Resistance |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ihold | Itrip | Operating | Interrupt | Imax | Pd | To Trip |  |  |  |  |
|  | (MA) | (MA) | (Vdc) | (Vrms) | (A) | Typ. | Current | Time | Rimin. | Rimax. | R1max |
|  |  |  |  |  |  | (W) | (A) | (Sec) | () | () | () |
| 250V40mA | 40 | 80 | 60 | 250 | 3.0 | 1.00 | 0.5 | 0.2 | 30 | 60 | 80 |
| 250v 60mA | 60 | 120 | 60 | 250 | 3.0 | 1.00 | 0.5 | 0.5 | 20 | 40 | 60 |
| 250v 80mA | 80 | 160 | 60 | 250 | 3.0 | 1.00 | 1.00 | 0.25 | 14 | 22 | 33 |
| 250v90mA | 90 | 180 | 60 | 250 | 3.0 | 1.00 | 1.00 | 0.5 | 10 | 20 | 31 |
| 250V110mA | 110 | 220 | 60 | 250 | 3.0 | 1.00 | 1.00 | 1.1 | 6 | 12 | 16 |
| 250v120mA | 120 | 240 | 60 | 250 | 3.0 | 1.00 | 1.00 | 1.2 | 6 | 11 | 16 |
| 250V 145mA | 145 | 290 | 60 | 250 | 3.0 | 1.00 | 1.00 | 2.5 | 3.5 | 6.5 | 12 |
| 250V 180mA | 180 | 360 | 60 | 250 | 10 | 1.8 | 3.00 | 1.5 | 1 | 3 | 5 |
| 250V200mA | 200 | 400 | 60 | 250 | 10 | 2.4 | 3.00 | 5 | 3 | 6 | 9 |
| 250V400mA | 400 | 800 | 60 | 250 | 10 | 2.8 | 3.00 | 8 | 1 | 3 | 5 |
| 250V600mA | 600 | 1200 | 60 | 250 | 10 | 3.2 | 3.00 | 10 | 0.6 | 2.0 | 4 |
| 250V800mA | 800 | 1600 | 60 | 250 | 10 | 3.6 | 3.00 | 20 | 0.4 | 1.0 | 3 |

V max  = Maximum operating voltage device can withstand without damage at rated current (Imax).

I max   = Maximum fault current device can withstand without damage at rated voltage (V max).

I hold   = Hold Current. Maximum current device will not trip in 25°C still air.

I trip    = Trip Current. Minimum current at which the device will always trip in 25°C still air.

Pd      = Power dissipation when device is in the tripped state in 25°C still air environment at rated voltage.

Ri min/max  = Minimum/Maximum device resistance prior to tripping at 25°C.

R1max  = Maximum device resistance is measured one hour post reflow.

CAUTION : Operation beyond the specified ratings may result in damage and possible arcing and flame.

Environmental Specifications

| Test |  |  |  | Conditions |  |  |  | Resistance change |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Passive aging |  |  |  | +85°C, 1000 hrs. |  |  |  | ±5% typical |  |  |
| Humidity aging |  |  |  | +85°C, 85% R.H. , 168 hours |  |  |  | ±5% typical |  |  |
| Thermal shock |  |  |  | +85°C to -40°C, 20 times |  |  |  | ±33% typical |  |  |
| Resistance to solvent |  |  |  | MIL-STD-202,Method 215 |  |  |  | No change |  |  |
| Vibration |  |  |  | MIL-STD-202,Method 201 |  |  |  | No change |  |  |
| Ambient operating conditions : - 40 °C to +85 °C |  |  |  |  |  |  |  |  |  |  |
| Maximum surface temperature of the device in the tripped state is 125 °C |  |  |  |  |  |  |  |  |  |  |

Ihold Versus Temperature

| Model | Maximum ambient operating temperature (Tmao) vs. hold current (Ihold) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | -40°C | -20°C | 0°C | 25°C | 40°C | 50°C | 60°C | 70°C | 85°C |

Soldering Parameters

Time

TP 260

100

25

Soldering

5Sea.MAX

Temperature(°C)

Gradual

Cooling

Pre-Heating

1 Minute Min.

| WAVE SOLDERING INFORMATIONS |  |
| --- | --- |
| Pre-Heating Zone | Max. ramping rate should not exceed 4℃/Sec. |
| Soldering Zone | Max. solder temperature should not exceed 260℃ |
| Cooling Zone | Cooling by natural convection in air. |
| ◎Specifications are subject to change without notice. |  |

Physical Dimensions(mm.)

| Model | A | B | C | D | E |
| --- | --- | --- | --- | --- | --- |
|  | Max. | Max. | Typ. | Min. | Max. |
| 250V040MA | 6.0 | 9.3 | 5.1 | 5.0 | 3.8 |
| 250V080MA | 6.0 | 9.3 | 5.1 | 5.0 | 3.8 |
| 250V090MA | 6.0 | 9.3 | 5.1 | 5.0 | 3.8 |
| 250V110MA | 6.5 | 10.0 | 5.1 | 5.0 | 3.8 |
| 250V120MA | 7.0 | 10.0 | 5.1 | 5.0 | 3.8 |
| 250V145MA | 7.0 | 10.0 | 5.1 | 5.0 | 3.8 |
| 250V180MA | 10.2 | 14.5 | 5.1 | 5.0 | 3.4 |
| 250V200MA | 10.5 | 17 | 5.1 | 5.0 | 3.8 |
| 250V400MA | 10.5 | 17 | 5.1 | 5.0 | 3.8 |
| 250V600MA | 16 | 18 | 5.1 | 5.0 | 4.5 |
| 250V800MA | 20 | 22 | 5.1 | 5.0 | 4.5 |